## Slide 1: Mechanistic Kinetic Modeling of Furfural Hydrodeoxygenation to Produce 2-Methylfuran in a Fixed Bed Reactor
Presented by:
Sayed Musaraf Ali
2022CHB1057
Guided by:
Dr. tarak mondal
- CP-303

## Slide 2: Introduction
MOTIVATION
Furfural is a key biomass-derived platform molecule obtained from lignocellulosic feedstocks.
Upgrading furfural to fuels enhances the value of renewable biomass resources.
Target product: 2-Methylfuran (2-MF)
High energy density biofuel
SIGNIFICANCE OF KINETIC STUDY
Helps identify rate controlling steps and adsorption effects
Provides mechanistic understanding beyond empirical correlations
Catalyst: CuFe₂O₄ (Copper Ferrite) + Cu/Fe2O3

## Slide 3: Project Objectives
Establish an empirical power-law kinetic model.
Develop a mechanistic Langmuir–Hinshelwood–Hougen–Watson (LHHW) model.
Estimate kinetic & thermodynamic parameters.
Validate models statistically.
Compare empirical (power law) and mechanistic (LHHW) kinetic models
Propose detailed reaction mechanism based on elementary surface reactions

## Slide 4: Kinetic Models Considered
  Overall FFR reaction:
  Overall FAL reaction:
Power Law Models : (is in excess)
Arrhenius:
Reference is taken at 230 K.
Total kinetic parameters estimated: 6 (2 , 2 Ea, 2 reaction orders).
This formulation enables parameter estimation by combining Partial pressure dependence and temperature dependence.

## Slide 5: Estimation of Kinetic Model Parameters
Power-law rate expression:
Used MATLAB lsqcurvefit for regression fitting.
  Multiple Linear Regression (per Temperature)
  Fits the power law form at each temperature separately:
ln(r​) = ln() + n.ln()
  Requires a second step (Arrhenius fit) to get activation energy .
The objective function is:
Minimize
Validate models (R², residuals, confidence intervals).
Correlation of Parameters

## Slide 6: Data Processing
Raw experimental data provided:
  Volumetric flow rate (mL/min)
  Temperature (°C)
  Conversion of Furfural (FFR)
  Yield of Furfuryl Alcohol (FAL)
  Yield of 2-Methylfuran (2-MF)
  Catalyst weight (W)
  5% FFR in IPA
Calculation of Molar Flow Rate (mol/h)
Rate of reaction of FFR (mol·h⁻¹·)
Partial Pressure Calculation

## Slide 7: RESULTS
FFR to FAL
FAL to 2MF
Parameters | Value | -95% CI | +95% CI
k_ref (mol/h.g.bar^n) | 0.087094 | 0.08328 | 0.09091
Ea (KJ/mol) | 42.80 | 39.08 | 46.52
n (FFR order) | 0.364 | NR | NR
RMSE | 0.002304 |  | 
Parameter | Value | -95% CI | +95% CI
k_ref (mol/h.g.bar^m) | 0.135041 | 0.09722 | 0.17286
Ea (KJ/mol) | 73.26 | 38.11 | 108.41
m (FAL order) | 0.533 | NR | NR
RMSE | 0.001437 |  | 

## Slide 8: Arrhenius Analysis
Slope = -E/R = -5148.358055
Intercept = = -2.440768
Slope = -E/R = -8811.724
Intercept = = -1.819507

## Slide 9: Correlation Matrix
FFR to FAL
FAL to 2-MF
Params | k_ref | Ea | n
k_ref | 1 | 0.0747 | 0.8824
Ea | 0.0747 | 1 | 0.5009
n | 0.8824 | 0.5009 | 1
Correlation | Interpretation | 
< 0.3 | Good | 
0.3–0.7 | Moderate | 
> 0.8 | Strong (problematic) | 
Params | k_ref | Ea | m
k_ref2 | 1 | 0.1666 | 0.994
Ea | 0.1666 | 1 | 0.2557
m | 0.994 | 0.2557 | 1

## Slide 10: Parity Plot -FFR to FAL

## Slide 11: Parity Plot - FAL to 2-MF

## Slide 12: LHHW Model Overview
Why go beyond Power Law?
Power law models provide good statistical fit but limited mechanistic insight
Cannot explain:
  Competitive adsorption
  Surface reaction mechanism
  Product inhibition
  Effect of site coverage
LHHW provides a mechanistic, surface-kinetics-based framework.
Used when:
  Rate-controlling step is surface reaction
  Reactants adsorb on active sites
  Surface coverage influences rate

## Slide 13: LHHW Model
Key Assumptions of LHHW :
  All reactants, intermediates, and products adsorb on the same type of catalyst active site (for Single Site).
  Hydrogen adsorb on the hydrogen active catalyst sites whereas others adsorb on the other organic catalyst active sites (for Dual Site).
  Molecular adsorption of Furfural, Furfuryl alcohol and 2-Methyl Furfuran.
  Hydrogen adsorbs dissociatively.
  Surface-reactions step are rate-controlling.
  Catalyst does not deactivate during experiments.
  Ideal-gas behaviour.
We have total of 2 Models (2 rate equations each)

## Slide 14: Elementary Reactions
Single Site RM Dual Site RM
RDS are reaction 3 and reaction 5

## Slide 15: LHHW Model
LH-I RM LH-II RM
Arrhenius Equation:
Van’t Hoff Adsorption Equation:
Total parameters estimated: 9 per model (2 , 2 and 5 ).

## Slide 16: KINETICS RESULT
Reaction Mechanism and Model | Rate Constant | k_ref (mol/h g-cat) | (-95%) CI | (+95%) CI | Ei (KJ mol) | -95% CI | +95% CI | RMSE | F-Test Statistics
LH-I | kc | 0.12215 | 0.04097 | 0.20333 | 34.31 | 15.42 | 53.20 | 0.003035 | (F=123.09), (p=0.0000)
Single Site | ke | 71.02 | 26.39 | 115.65 | 37.02 | 12.84 | 61.20 | 0.000542 | (F=123.09), (p=0.0000)
LH-II | kc | 0.02253 | 0.02035 | 0.02471 | 37.73 | 29.88 | 45.58 | 0.003756 | (F=74.08), (p=0.0000)
Dual-Site | ke | 123.72 | 74.12 | 173.32 | 60.13 | 29.80 | 90.46 | 0.000583 | (F=74.08), (p=0.0000)

## Slide 17: ARRHENIUS ANALYSIS LH-I
Slope = -E/R = -4048.4
Intercept = = -2.1035
Slope = -E/R = -4436.7
Intercept = = 4.2616

## Slide 18: ARRHENIUS ANALYSIS LH-II
Slope = -E/R = -4551.3536
Intercept = = -3.79086
Slope = -E/R = -7234.96573
Intercept = = 4.81989

## Slide 19: THERMODYNAMICS RESULTS
CHANGE IN ENTROPY OF ADSORPTION ()
 | LH-I |  |  |  | LH-II |  |  |  | 
Adsorption Constant | (J/mol K) | (-95%) CI | (+95%) CI | t-Statistic / p-Value | (J/mol K) | (-95%) CI | (+95%) CI | t-Statistic / p-Value | (KJ/mol)
K_FFR | -96.03 | NR | NR | 0.05520 /0.9561 | -70.28 | -79.22 | -61.34 | 15.48/ 0.0000 | -51.5
K_H | -133.75 | NR | NR | 0.03700 / 0.9706) | -30.51 | -36.35 | -24.67 | 10.254/ 0.0000 | -50
K_FAL | -31.81 | NR | NR | 0.015300 /0.9878 | -32.53 | -37.68 | -27.38 | -12.852/ 0.0000 | -28.9
K_MF | -84.27 | NR | NR | 4.8892E-8/1.0000 | -17.57 | NR | NR | -0.2821/ 0.7783 | -15
K_H2O | -84.80 | NR | NR | -0.0480 /0.9618 | -38.87 | -80.71 | 2.97 | -1.5349/ 0.1274 | -52
 | LH-I |  |  |  | LH-II |  |  |  | 
Adsorption Constant |  | (-95%) CI | (+95%) CI | t-Statistic / p-Value |  | (-95%) CI | (+95%) CI | t-Statistic / p-Value | 
K_FFR | -96.03 | NR | NR | 0.05520 /0.9561 | -70.28 | -79.22 | -61.34 | 15.48/ 0.0000 | -51.5
K_H | -133.75 | NR | NR | 0.03700 / 0.9706) | -30.51 | -36.35 | -24.67 | 10.254/ 0.0000 | -50
K_FAL | -31.81 | NR | NR | 0.015300 /0.9878 | -32.53 | -37.68 | -27.38 | -12.852/ 0.0000 | -28.9
K_MF | -84.27 | NR | NR | 4.8892E-8/1.0000 | -17.57 | NR | NR | -0.2821/ 0.7783 | -15
K_H2O | -84.80 | NR | NR | -0.0480 /0.9618 | -38.87 | -80.71 | 2.97 | -1.5349/ 0.1274 | -52

## Slide 20: CORRELATION
LH-I | dS1 | dS2 | dS4 | dS6 | dS7
dS_FFR | 1.000 | 1.000 | 1.000 | -0.042 | -1.000
dS_H | 1.000 | 1.000 | 1.000 | -0.042 | -1.000
dS_FAL | 1.000 | 1.000 | 1.000 | -0.042 | -1.000
dS_MF | -0.042 | -0.042 | -0.042 | 1.000 | 0.042
dS_H2O | -1.000 | -1.000 | -1.000 | 0.042 | 1.000
LH-II | dS1 | dS2 | dS4 | dS6 | dS7
dS1 | 1.000 | -0.518 | 0.036 | -0.032 | 0.067
dS2 | -0.518 | 1.000 | -0.169 | -0.006 | -0.051
dS4 | 0.036 | -0.169 | 1.000 | 0.664 | -0.756
dS6 | -0.032 | -0.006 | 0.664 | 1.000 | -0.977
dS7 | 0.067 | -0.051 | -0.756 | -0.977 | 1.000

## Slide 21: PARITY PLOT LH-I

## Slide 22: Parity Plot LH-II

## Slide 23: HEAT AND MASS TRANSFER LIMITATION

## Slide 24: FINDINGS
Reaction Step | Present Work (LH-II) | Literature Trend | Interpretation
Furfural → FAL (Hydrogenation) | 37.73 kJ/mol | Lower Ea reported for carbonyl hydrogenation | Kinetically easier step
FAL → 2-MF (Hydrodeoxygenation) | 60.13 kJ/mol | Higher Ea reported for HDO reactions | Rate controlling / energy demanding step
Consistent with Previous Studies
  Cu-based catalysts favor sequential:
  FFR → FAL → 2-MF
  Furfuryl alcohol identified as major intermediate.
Thermodynamic Consistency
  Adsorption Parameters Negative ΔS → Reduced randomness during adsorption
  Physically meaningful adsorption behavior obtained

## Slide 25: CONCLUSION
Developed kinetic models for furfural hydrodeoxygenation using: Power Law model and Langmuir–Hinshelwood (LH) model.
Dual-site LHHW model (LH-II) showed: Better thermodynamic consistency, lower parameter correlation and improved statistical reliability.
Activation energy results indicated:
  Furfural hydrogenation is kinetically easier
  Deoxyhydrogenation (FAL → 2-MF) is the more energy-demanding step
Negative ΔS values confirmed: Exothermic adsorption and Reduced randomness during adsorption.
Heat and mass transfer analyses confirmed:
  Absence of transport limitations
  Observed rates represent intrinsic kinetics
Developed model successfully explained:
  Adsorption effects
  Surface reaction mechanism
  Selective formation of 2-Methylfuran (2-MF)

## Slide 26: References
https://www.sciencedirect.com/science/article/pii/S0016236122035359
https://www.sciencedirect.com/science/article/pii/S0016236124002485
https://www.sciencedirect.com/science/article/pii/S2213343716303736
https://pubs.acs.org/doi/full/10.1021/ acs.iecr.5b03828
H. Scott Fogler. Elements of Chemical Reaction Engineering. 5th Edition.